VMZINC flat lock wall cladding on vented galvanized steel deck – 
April 26
H74 Zinc strip / sheet coverings / flashings

To be read with preliminaries / general conditions
TYPES OF ZINC WORK
130
Main Cladding
· 
Cladding system:  VMZINC Flat lock vertical cladding.seam cladding (horizontal, vertical and diamond shaped panels) for vertical walls and soffits.
· Substrate: 0.7mm min galvanised steel deck fixed to a metal framing system. The galvanised steel deck must have dimensions, allowing clips to be attached at the required spacings. The galvanised steel deck can only be used on vertical surfaces. For all surfaces such as sills, parapets, etc the substrate must be continuous.  The metal framing system, should create a minimum 38mm vented airspace, between the steel deck and the insulation. The galvanized steel deck and cladding rails should all be A1 or A2 according to EN13501-1. 
· Vapour control layer as per requirements.

· Metal Framing System as per requirements
· Insulation as per requirements but A1 or A2 according to EN13501-1. 
· Zinc:  As clause 520.

· Finish:  VMZINC in QUARTZ-ZINC, ANTHRA-ZINC, AZENGAR or PIGMENTO Grey, Red, Green, Blue, Grey, Brown, Storm Grey or Charcoal Blue. Non-vertical areas to be VMZINC PLUS in the appropriate finish. All be A1 or A2 according to EN13501-1. 
· Thickness: 0.7mm, 0.8mm or 1mm depending on panel size.
· Longitudinal joints:  25mm single welts, in accordance with manufacturer’s recommendations.  
· Spacing:  not more than 3000mm and in accordance with design and wind loadings. 

· Cross joints:  25mm single welts, in accordance with manufacturer’s recommendations.  
· Spacing, panels to be no longer than 3m. Only spacing in one direction can be over 600mm
· The vented cavity should be fire stopped wherever necessary with continuous vertical fire stops or horizontal intumescent fire stops allowing a minimum 25mm vented cavity.
· The Zinc should have an Environmental Product Declaration according to EN15804 indicating a service life of 100years.
340
Vented base detail

•
Eaves zinc:  As clause 520. 


-  Finish:  VMZINC in QUARTZ-ZINC, ANTHRA-ZINC, AZENGAR or PIGMENTO Red, Green, Blue, Grey, Brown, Storm Grey or Charcoal Blue. 


-  Thickness:  0.8mm. 

•
Joints:  Spacing:  2m.


•
Continuous drip 10mm linear vent opening
470
Vented Parapet 

•
Ridge:  As clause 520. 


-  Finish:  VMZINC in QUARTZ-ZINC, ANTHRA-ZINC, AZENGAR or PIGMENTO Red, Green, Blue, Grey, Brown, Storm Grey or Charcoal Blue. 

-  Thickness:  0.8mm. 

•
Joints:  Spacing:  2m.


•
Overlap between tray and parapet at least 60mm with 10mm linear vent opening.

GENERAL REQUIREMENTS/PREPARATORY WORK
510
WORKMANSHIP GENERALLY

•
Standard:  Generally to CP 143-5.


•
Fabrication and fixing:  To provide a secure, free draining and completely weather tight installation.
· Operatives:  Trained in the application of zinc coverings/flashings by participation in a VMZINC training course.  Submit records of experience on request.  VMZINC at Work installers offer evidence of successfully completed projects, records of VMZINC training and extended material warranties.


•
Measuring, marking, cutting and forming:  Prior to assembly wherever possible. 

•
Metal temperature:  Do not form zinc when the metal temperature is below 7˚C. (10˚C for PIGMENTO).

•
Marking out:  With pencil, chalk or crayon.  Do not use scribers or other sharp instruments without approval. 

•
Folding: With mechanical or manual presses to give straight, regular and tight bends, leaving panels free from ripples, kinks, buckling and cracks.  Use hand tools only for folding details that cannot be pressed. The minimum bending radius is thickness x 2 (x 3 for PIGMENTO).

•
Sharp metal edges:  Fold under or remove as work proceeds. 

•
Sealants:  Do not use in joints to attain waterproofing. 

•
Solder:  Use only where specified. 

•
Finished zinc work:  Fully supported, adequately fixed to resist wind uplift and able to accommodate thermal movement without distortion or stress. 

•
Protection:  Prevent staining, discolouration and damage by subsequent works.  All instructions and recommendations contained in the guidelines for design and specification and VMZINC General Technical Recommendation of VMZINC standing seam facades to be applied.  Plastic film must be removed within 2 months of installation and in such a way so as not to trap water between the partially removed film and the zinc. 
520
ZINC STRIP/SHEET

•
Zinc-titanium-copper alloy: 



-  To BS EN 501 and BS EN 988. 


•
Zinc manufactured following ISO 14001 (environmental management) and ISO 9001 (quality management). 


-  Stamped or labelled with type, finish and thickness.  

•
Installed material must come from the same batch.



-  Zinc to be coated on underside with a protective 60 micron lacquer for non-vertical surfaces.

•
Manufacturer:



-  VMZINC Suite 1 Ground Floor Prince of Wales House 3 Bluecoats Avenue Hertford  SG14 1PB



   Tel:  01992 921 300   Email: vmzinc.uk@vmbuildingsolutions.com   Web:  www.vmzinc.co.uk



-  Product reference:



   VMZINC and VMZINC PLUS in QUARTZ-ZINC, ANTHRA-ZINC, AZENGAR or PIGMNETO Red, Green, Blue, Grey, Brown, Storm Grey or Charcoal Blue. 
535
INTEGRITY OF ZINC

•
Requirement:  Design coverings/flashings and methods of attachment to prevent loss of weather tightness and permanent deformation due to wind pressure or suction. 

•
Wind loads:  Calculate to BS 6399-2. 
555
LAYOUT

•
Setting out of longitudinal and cross joints:  Submit proposals.

610
SUITABILITY OF SUBSTRATES

•
Condition:  Dry and free of dust, debris, grease and other deleterious matter.
620
PREPARATION OF ANY EXISTING TIMBER SUBSTRATES

•
Remedial work: Adjust boards to level and securely fix. Punch in any protruding fasteners and plane or sand to achieve an even surface. 

•
Defective boards:  Give notice. 

•
Moisture content:  Not more than 22% at time of covering. 
FIXING ZINC
710
FIXINGS FOR CLIPS

· Stainless steel or Galvanised steel (not in a coastal environment) 
· Flat head screws or ringed shanked nails.
715
SECURING CLIPS


•
Stainless Steel, Zinc or Galvanised steel (not in a coastal environment). 

•
Fixing:  Secure each clip to substrate with two fixings. 

•
Each clip to withstand a pulling force of 50 daN.


•
Minimum of 4 clips per panel. 


•
Typical spacing:  clip at least every 330m.

760
CONTINUOUS CLIPS


Material:  Zinc of same thickness as that being secured. 

•
Dimensions: 


-  Width:  To suit detail. 


-  Length:  Not more than 1.8m. 

•
Fixing:  To substrate at 200mm centres.  Welt edge of strip/sheet being fixed to continuous clip and dress down. 
810
FORMING DETAILS

•
Folds and welts:  Form without thinning, or splitting the strip/sheet.

•
Thermal movement:  Form details with appropriate allowance for movement, without impairment of security at full expansion or contraction.
825
SOLDERING


•
All zinc must be cleaned back to its natural state.

•
The protective coat on the underside of the upper panel must be removed over a width of 20mm either chemically, using DECALAQ, or mechanically, using a 3 MTM RolocTM  Bristle Disc brush mounted on a small disc sander.

•
The pre-weathering must be removed from the parts to be soldered.  ZINN7 (flux) to be applied to allow spot soldering with solder (40% tin 60% lead)   ZINN7 applied over whole length of joint and then soldered.  Wipe clean
IMPORTANT
All instructions and recommendations within VM Building Solutions brochures should be applied. In particular, VMZINC Facades, VMZINC Standing Seam Installation Guide and VMZINC General technical recommendations should be consulted. All literature is available online at www.vmzinc.co.uk
